| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION |
| --- |
| District: Fort St. John, BC | Skid No. |
| Facility: Sikanni Compressor Station | Location (LSD): b-10-L / 94-G-03 |
| Vessel Name Equipment Number: Heat Medium Heater |
| Orientation: Horizontal |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. RAE 3643 | CRN Number: F-1500.21 |
| Vessel serial number: 966-80-85 | Size: 42 in. x 120 in |
| Shell thickness: Not Stated | Shell material: Not Stated |
| Head thickness: Not Stated | Head material: Not Stated |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: | Operating pressure | Shell: N/S |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: | Operating temperature | Shell: -10 - 115°C |
|  | Tubes: | 25°C | Tubes: |
| X-ray: RT 1 | Heat treatment: Not Stated |
| Code parameters: ASME VIII, Div 1 | Coated: No |
| Manufacturer: Not Stated | Year built: 1985 |
| Corrosion allowance: Not Stated | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture | Model # | Serial # | Set Pressure (kPa) | Capacity (scfm) | Service Date |
| CRN # | Service By | Block Valve | Location | Size | Code Stamp |  |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas | Water |
| Amine | LPG | Condensate | Air | Glycol X |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | Vessel not insulated. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) |  | X |  |  | Paint peeling from top shell of vessel. Approximately 30% of shell surface has peeled |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks |
| Saddle Assess condition of paint, fire protection, and concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Paint peeling from base of saddles – no corrosion. No leaks No buckling or dents No ground wire attached. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Anchor bolts are secure to skid frame |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, and describe any hazards. |  |  |  | X |  |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | No deflection. No gussets – studs fully engaged to nuts on flanges. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Gauge is visible but glass is cloudy, working and no leaks -10 - 115°C |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Piping is well supported; all clamps, supports and shoes are in place. Piping is insulated - no damage present. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | No leaks Valve are properly supported |
| PSV Ensure PSV is set at pressure at or below that of vessel. |  |  |  | X | No PSV |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | No NDE inspections at this time. |
| Other |  |  |  |  |  |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1. Attach ground wire to vessel or skid. Summary: This Vessel is in good overall condition, visual external carried out. Vessel is fit for service |

Inspected By: Gerry Avery   									Date:  Aug.10, 2006