| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION |
| --- |
| District: Fort St. John BC | Skid No. |
| Facility: Inga Unit #2 Compressor | Location (LSD): 03-31-86-23-W6M |
| Vessel Name Equipment Number: VRU Inlet Separator |
| Orientation: Vertical |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. C72971 | CRN Number: Non Code |
| Vessel serial number: 12911-149 | Size: 12 in. x 60 in. |
| Shell thickness: 9.5 mm | Shell material: SA-106-B |
| Head thickness: 7.9 mm | Head material: SA-516-70 |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 103 Kpa | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 149 Deg C | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: Nil | Heat treatment: Nil |
| Code parameters: Non Code | Coated: No |
| Manufacturer: Eagle Pump & Compressor Ltd. | Year built: 1996 |
| Corrosion allowance: 1.6 mm | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture | Model # | Serial # | Set Pressure (kPa) | Capacity (scfm) | Service Date |
| 27945 | Farris | 2850-1000 | CE-315417-20 | 103 | 161 | 06/2007 |
| CRN # | Service By | Block Valve | Location | Size | Code Stamp |  |
| 0G2367.5C | IPV | No | Inlet piping | 1”x 1.5” | UV |  |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet | Sour X | Oil | Gas X | Water |
| Amine | LPG | Condensate | Air | Glycol |
| Other (Describe): |

Job # 10.110194

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | No insulation. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint is in good overall condition – No corrosion or exposed metal. – No previous corrosion. |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaking detected. |
| Saddle Assess condition of paint, fire protection, and concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Skirt: Vessel is firmly bolted to skid floor. No buckling or dents. No corrosion at attachment welds to vessel. Ground cable secured to vessel skid unit. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Vessel is firmly anchored to skid floor. No signs of deformation. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X | None. |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, and describe any hazards. |  |  |  | X | None. |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | All threads connections fully engaged. No deflection – no leaks. No gussets. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Gauges are visible, appears to be functional, no leaks and suitable for range of MAWP. No Pressure gauge. Temperature gauge: -20 to 120 deg C / 30 deg C @ gauge. |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Well supported – no deflection – all clamps and shoes in place. Piping is painted and in good condition – no surface corrosion found. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | Well supported – no leaks. |
| PSV Ensure PSV is set at pressure at or below that of vessel. | X |  |  |  | Located on Inlet piping - set at the vessels MAWP. Discharge piping is the same size as the outlet to PSV. No block valve present. Seal is intact. PSV vents to flare. |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic thickness survey carried out-pipe metal thickness detected below nominal minus corrosion allowance. UT point 3005 (6” Elbow) – nominal thickness is 7.1mm / min thickness is 6.0mm / T min thickness is 1.6mm. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1. No recommendations at this time. Summary: This vessel is in good over all condition, visual external and ultrasonic thickness survey carried out-pipe metal thickness detected below nominal minus corrosion allowance. Long term corrosion rate based on greatest thickness loss – shell – nominal thickness is 9.5 mm / min thickness is 8.8 mm / T min thickness is 1.6 mm = corrosion rate of .046 mm per year = Retirement date of 2167. Vessel is fit for service. |

Inspected By: Joseph Holdstock								                      Date: April-07-2011.

| LSD Location | Site overview |
| --- | --- |
| Data plate | Overview |
| Base anchored securely | Lower shell |
| PSV service tag | PSV service tag |
| PSV Data plate | Temperature gauge |