| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION Job# 05.003230 |
| --- |
| District: Grande Prairie, AB | Skid No. |
| Facility: Berland River Gas Plant | Location (LSD): 16-15-59-24 W5M |
| Vessel Name Equipment Number: Inlet Separator |
| Orientation: Horizontal |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. A 496381 | CRN Number: R 1481.21 |
| Vessel serial number: PE 7964 | Size: 42 in x 12 ft |
| Shell thickness: 25.4 mm | Shell material: SA 516-70N |
| Head thickness: 25.4 mm | Head material: SA 516-70N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 5688 kPa | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 38°C | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: RT-2 | Heat treatment: No |
| Code parameters: ASME VIII, Div 1 | Coated: No |
| Manufacturer: Penfabco Ltd. | Year built: 2003 |
| Corrosion allowance: 1.6 mm | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| Tag Number(s) | Set Pressure kPa | CRN # | Manufacturer /Model / Serial# and Code Stamp | Capacity (Scfm) | Size | Set Date |
| PSV 1 | 5516 | OG 0703.9C | Crosby //JOS – E – 45/J // C05-04-239 // UV NB | 12563 | 2 in x 3 in | 06/09 |
| PSV 2 | 4964 | OG 1316.2C | Taylor // T 8200-1 // 7546-8 // UV NB | 2615 | 2 in x 3 in | 06/09 |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas X | Water X |
| Amine | LPG | Condensate X | Air | Glycol |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of  CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | This vessel is not insulated. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint is in good condition, no exposed metal – no previous corrosion. |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks detected. |
| Base/Skirt Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Saddle – no distortion to saddle – no corrosion at saddle to shell welds – no leaks. Paint is in good condition – no exposed metal. Skid has ground wire attached. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Saddles are firmly bolted to skid deck. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X | Skid deck is metal. |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, describe any hazards. |  |  |  | X | None |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | Threaded nozzle joints are fully engaged – no leaks. Nozzles are not gusseted Studs fully engaged to nuts – no short bolts No deflection. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Pressure gauge: 0 to 600 PSI. |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Paint in good condition – no exposed metal. Piping is well supported, no deflection, all clamps and supports are in place. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | Valves are supported – no leaks. |
| PSV Ensure PSV is set at pressure at or below that of vessel. | X |  |  |  | Located on top shell – set below MAWP of vessel. Discharge piping is same size as valve outlet. Valve is properly supported and routed. PSV seal in place. No block valve. |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) |  |  |  |  | Ultrasonic thickness survey carried out in 2003 – pipe metal thickness detected below nominal minus corrosion allowance. Thickness calculations carried out to ensure sufficient metal exists for safe operation. |
| Other Observations: See internal inspection for recommendations and summary. |

Inspected By: Dellas Wiedman                                                                                                                                 Date:  June 10, 2009

| Internal Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Coating Assess coating. Describe area coated, general condition of coating. |  |  |  | X | No coating. |
| Anodes. How many, type, condition. % consumed. Are they being replaced? |  |  |  | X | No anodes |
| Internal Piping Is there any? If so, carbon or stainless steel. Describe condition, dents, corrosion, erosion, etc. Ensure supports are secure and any bolts are suitable for future use. | X |  |  |  | Heat Medium coil: Good condition – soiled and scaled – no pitting. |
| Trays How many? Type of material. Are valves in place. Check for erosion/ corrosion; wear on tray valve legs. Cleanliness? |  |  |  | X | No trays. |
| Baffles, deflector plates, etc. If present, describe condition. Look closely at welds attached to vessel wall. | X |  |  |  | Surge weir and condensate weirs are in place. |
| East Head Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head) | X |  |  |  | Limited viewing – weir is welded in place on the West end of the separator and only 10 inches of space is above the weir. Good condition – no obvious corrosion or pitting – this is the condensate side of the vessel. |
| West Head – man way access Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head) | X |  |  |  | Hard bonded scale to most of surface area – no corrosion or pitting. |
| Shell Sections Record number of shell sections. Record location, size and depth of all erosion, corrosion or mechanical damage. Describe general condition. If any corrosion greater than corrosion allowance is observed in either shell or head, discuss with Chief Inspector before closing vessel. | X |  |  |  | 2 can sections – no corrosion or pitting detected – light scaling to upper phase. |
| Demister pad Is it in place? Is it clean? If any corrosion is apparent in vessel, lift pad and check top head for corrosion. | X |  |  |  | Gage is intact and in place – no distortion. Mistex pad is not viewable as the weir made it impossible to see – there was no evidence of moisture carry over in the compression system so its assumed to be in place and doing its job. |
| Welds Inspect all welds, including attachment welds. Record all service-related damages and if there is any discuss with Chief Inspector before closing. | X |  |  |  | Good condition, no corrosion or pitting. |
| Repairs Required. If yes, ensure procedure and copy of AB 40 is on file, and one sent to local ABSA, and Chief Inspector |  |  |  | X | No repairs required. |
| NDE Was any NDE done. ( MI coordinator to review results) |  |  |  | X | No internal NDE at this time. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Other Observations: Recommendations: 1. Replace pressure gauge. Summary: This vessel is in good overall condition, visual internal and external carried out. Magnetic Particle Inspection carried out on all “T” intersects and nozzle welds – no cracking detected. No items of concern. Vessel is fit for service |

Inspected By: Dellas Wiedman                                                                                                                                 Date:  June 10, 2009

Photo Table

| Data Plate | Overview |
| --- | --- |
| Over view – vessel piping | Pressure gauge |
| PSV attachment area | Bolting |
| Man way | Man way |
| Condensate weir | Heat medium coil |
| Thermal well | Head |
| Surge weir |  |