| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION Job # 05.00 |
| --- |
| District: Fort St. John BC. | Skid No. |
| Facility: Bucking Horse | Location (LSD): d-44-A/94-G-10 |
| Vessel Name Equipment Number: Test Separator |
| Orientation: Horizontal |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. A242825 | CRN Number: F 7742.1 |
| Vessel serial number: 881029 | Size: 54 in. x 10 ft. |
| Shell thickness: 34.9mm | Shell material: SA 516-70N |
| Head thickness: 34 mm | Head material: SA 516-70N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 1407 PSI | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 100 Deg F | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: RT1 | Heat treatment: yes |
| Code parameters: ASME VIII, Div 1 | Coated: not stated |
| Manufacturer: I.P.Constructors | Year built: 1988 |
| Corrosion allowance: 3.2mm | Manway: no |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture | Model # | Serial # | Set Pressure (kPa) | Capacity (scfm) | Service Date |
| CRN # | Service By | Block Valve | Location | Size | Code Stamp |  |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas | Water |
| Amine | LPG | Condensate | Air | Glycol |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. | X |  |  |  | No damage present- sealed around nozzles and saddles. No egress of moisture. Straps are secure and in place. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint in good overall condition – No exposed metal. |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks observed. |
| Saddle/Skirt Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Saddle: welded directly to skid frame. Skid welded to pilings No buckling or dents. No corrosion at attachment welds to vessel. Ground wire attached to skid and pilings. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Anchor bolts are securely fastened. No deformation. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, describe any hazards. |  |  |  | X |  |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | Stud threads are fully engaged to nuts. No leaks observed. No damage or deflections. Nozzles are not gusseted. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Clear and clean- no leakage. Not suitable for range of MAWP/temperature of vessel. Pressure gauge 0 – 800 PSI. |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Piping is well supported – all clamps and supports are in place. No structural overloads or deflections. Paint in good condition- no exposed metal. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | No leaks are visible- Valves are supported properly. |
| PSV Ensure PSV is set at pressure at or below that of vessel. |  |  |  | X | No PSV |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic thickness survey carried out – no metal thickness detected below nominal. |
| Other |  |  |  |  |  |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: No recommendations at this time Summary: Vessel is in overall good condition. Visual inspection and ultrasonic corrosion survey performed—No metal thickness detected below nominal minus corrosion allowance. Vessel is fit for service. |

Inspected By: Gerry Avery			                                                        Date: January 13, 2009

Photo Table

| LSD | vessel data plate |
| --- | --- |
| vessel overview | vessel pressure gauge |