| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION |
| --- |
| District: Fort St. John, B.C. | Skid No. |
| Facility: Helmet Compressor Station | Location (LSD): a-71-G / 94-P-10 |
| Vessel Name Equipment Number: #2 Dehydration Tower |
| Orientation: Vertical |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. A 2877363 | CRN Number: H-3319.1 |
| Vessel serial number: 93G-4948-01 | Size: 36in x 38ft |
| Shell thickness: 44.4mm | Shell material: SA 516 70N |
| Head thickness: 41.8mm | Head material: SA 516 70N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 9756 kPa | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 66°C | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: RT-1 | Heat treatment: HT |
| Code parameters: ASME VIII, Div 1 | Coated: No |
| Manufacturer: Alco Gas & Oil | Year built: 1993 |
| Corrosion allowance: 3.2mm | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture | Model # | Serial # | Set Pressure (kPa) | Capacity (scfm) | Service Date |
| Inaccessible |  |  |  |  |  |  |
| CRN # | Service By | Block Valve | Location | Size | Code Stamp |  |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas X | Water |
| Amine | LPG | Condensate | Air | Glycol X |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X |  |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint is in good condition, no loose or flaking paint. |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks found. |
| Saddle Assess condition of paint, fire protection, and concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | No distortion or corrosion. Skid grounded |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. |  |  | X |  | 1 of 8 base bolts missing. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, and describe any hazards. |  |  |  | X |  |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? |  |  |  |  | No deflection, studs fully engaged to nuts. No gussets. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. |  |  |  |  | Pressure gage: 0 to 3000 psi operating at 500 psi. Temp gage: 10 to 260°C operates at 35°C |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | No deflection - visible clamps in place. Paint in good condition. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | No leaks found |
| PSV Ensure PSV is set at pressure at or below that of vessel. | X |  |  |  | PSV is not accessible without man lift – but is scheduled for servicing in 2006 so we will get the info from Unified in Ft Nelson. |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic thickness survey carried out-no metal thickness detected below nominal minus corrosion allowance. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendation: No recommendations at this time. Summary: This vessel is in good over all condition, ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance. Vessel is fit for service. |

Inspected By: Len Semanuik								                           Date: Jan 10/2006

###### A 2877363