| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION Job # 05.003373 |
| --- |
| District: Fort St John, BC | Skid No. |
| Facility: Graham Compressor Station | Location (LSD): C-76-K / 94-B-8 |
| Vessel Name & Equipment Number: Inlet Separator V-005 |
| Orientation: Horizontal |
| Status: In service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| Registration Number A 454381 | CRN Number P-0334.21 |
| Vessel serial number: 2000-6332-01 | Size: 66 in x 24 ft |
| Shell thickness: 76.4 mm | Shell material: SA 516 70N |
| Head thickness: 73.6 mm | Head material: SA 516 70N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 1332 PSI | Operating pressure | Shell: 150 PSI |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 200 deg F | Operating temperature | Shell: 70 deg F |
|  | Tubes: |  | Tubes: |
| X-ray: RT 1 | Heat treatment: HT |
| Code parameters: ASME VIII, Div I | Coated: DEVOE 253 |
| Manufacturer: Alco Gas & Oil | Built: 2000 |
| Corrosion allowance: 3.2 mm | Manway: Yes |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag no. | Manufacture | Model | Serial number | Set Pressure | Capacity | Size |
| N/S | Farris | HB13-120 | 420527-1-A11 | 1332 PSI | 20300 Scfm | 2” x 3” |
| Service By | Date | Block Valve | CRN number | Code Stamp | Location |  |
| Dalco | July 2009 | Yes In & out; locked Open | OG2369.5C | UV NB | Top Shell |  |
| SERVICE CONDTIONS-INDICATE ALL THAT APPLY |
| Sweet | Sour X | Oil | Gas X | Water X |
| Amine | LPG | Condensate X | Air | Glycol |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of  CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

### A 454381

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | No Insulation Present |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint in good condition no exposed metal present. |
| Leakage: Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leakage at flanges, weep holes or threaded joints. |
| Saddle: Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Saddle is firmly bolted to floor Paint in good condition. No corrosion, buckling or dents present. No leaking from attachment welds. Attachment is acceptable Ground is connected to skid. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Saddle firmly bolted to floor No signs of cracking or deformation. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, describe any hazards. | X |  |  |  | Ladder and platform is in good condition. One broken ladder rung noted. |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | Stud threads are fully engaged. No leaks-damage or deflections. Nozzles are not gusseted Paint in good condition. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Gauges are clear, clean and visible No leakage. Temperature Gauge (0 deg F – 250 deg F) Pressure gauge (0-3000 PSI) |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Piping is well supported – loose clamps present see photos. Supports are in place. No structural overloads or deflections. Corrosion occurring to 10% primarily under and around pipe support clamps. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | No leaks are visible. Valves are supported properly. |
| PSV Ensure PSV is set at pressure at or below that of vessel. Discharge piping is same size as inlet to valve and is properly supported and routed. Ensure no block valves between psv and vessel or if there are they are locked open. | X |  |  |  | Set at MAWP of vessel. PSV Discharge piping is larger than inlet piping. PSV seal in place – Inlet & Outlet block valve present wire locked open. Location: Top Shell |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic corrosion survey carried out, piping metal thickness detected below nominal minus corrosion allowance – pitting clusters. Calculations carried out to ensure sufficient metal exists for safe operation. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1) Review UT corrosion survey data pertaining to external vessel piping – water drain piping detected with pitting. 2. Tighten clamps on drain piping. Summary: This vessel is in good condition, ultrasonic corrosion survey carried out, piping metal thickness detected below nominal minus corrosion allowance – pitting clusters. Calculations carried out to ensure sufficient metal exists for safe operation. Vessel is fit for service |

Inspected By:  D. Wiedman / Matt Heatcoat                                                                                                               Date: Oct 15 – 2008

| Internal Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Coating Assess coating. Describe area coated, general condition of coating. |  |  |  | X | This vessel is 100% internally coated and is in good overall condition. |
| Anodes. How many, type, condition. % consumed. Are they being replaced? |  |  |  | X | None |
| Internal Piping Is there any? If so, carbon or stainless steel. Describe condition, dents, corrosion, erosion, etc. Ensure supports are secure and any bolts are suitable for future use. |  |  |  | X | None. |
| Trays How many? Type of material. Are valves in place? Check for erosion/ corrosion; wear on tray valve legs. Cleanliness? |  |  |  | X | None. |
| Baffles, deflector plates, etc. If present, describe condition. Look closely at welds attached to vessel wall. | X |  |  |  | Surge weir plate securely welded in place. – No mechanical damage found. |
| South Head Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head) | X |  |  |  | This head is fully coated & is in good overall condition – no failed areas. No mechanical damage. |
| North Head Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head) | X |  |  |  | This head is fully coated & is in good overall condition – no failed areas. No mechanical damage. |
| Shell Sections Record number of shell sections. Record location, size and depth of all erosion, corrosion or mechanical damage. Describe general condition. If any corrosion greater than corrosion allowance is observed in either shell or head, discuss with Chief Inspector before closing vessel. | X |  |  |  | Three shell sections were found to form this vessel. Shell is fully coated & in good overall condition – no failed areas. No mechanical damage was found. |
| Demister pad Is it in place? Is it clean? If any corrosion is apparent in vessel, lift pad and check top head for corrosion. | X |  |  |  | Demister vane pack was firmly intact & reasonably clean. |
| Welds Inspect all welds, including attachment welds. Record all service-related damages and if there is any discuss with Chief Inspector before closing. | X |  |  |  | All visible welds appear to be in good overall condition. |
| Repairs Required. If yes, ensure procedure and copy of AB 40 is on file, and one sent to local ABSA, and Chief Inspector |  |  |  | X | None. |
| NDE Was any NDE done. (MI coordinator to review results) | X |  |  |  | No NDT was performed inside this vessel. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1.No recommendations at this time. Summary: This vessel is in good overall condition, visual internal / external carried out – internal is coated with epoxy – no failed areas of coating. Vessel is fit for service. |

Inspected By: Joe Holdstock                                                                                                                               Date: July-08– 2009

| Data Plate | Data |
| --- | --- |
| Temperature Gauge | Pressure gauge |
| Overview | Overview |
| Overview | Overview |
| Loose clamp | Loose clamp |

| Broken ladder rung | PSV |
| --- | --- |
| PSV Data Plate |

| South end | Surge Weir Plate |
| --- | --- |

| South Head Overview – Stains present | Upper shell Overview |
| --- | --- |
| Lower shell | Lower shell |
| Water Boot | Demister Vane Pack |

| Lower Shell Overview – stains present | North Head Overview – stains present |
| --- | --- |