| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION Job: 10.113217 |
| --- |
| District: Fort St. John BC. | Skid No. |
| Facility: Cypress Gas Plant | Location (LSD): b-99-C-94-B-16 |
| Vessel Name Equipment Number: Inlet Separator |
| Orientation: Horizontal |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. A2564852 | CRN Number: H7272.21 |
| Vessel serial number: TW89J022 | Size: 54 in. X 12 ft. |
| Shell thickness: 57mm | Shell material: SA 516-70N |
| Head thickness: 56.4mm | Head material: SA 516-70N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 1350 PSI | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 151 Deg F. | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: RT 1 | Heat treatment: HT |
| Code parameters: ASME VIII Div 1 | Coated: Yes |
| Manufacturer: Tyson’s Welding. | Year built: 1989 |
| Corrosion allowance: 3.2mm | Manway: Yes |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture / Model / Serial | Set Pressure (PSI / kPa) | Capacity (scfm) | Size | Block Valve | Location | Service by Date |
| 14836 F | Consolidated//1912JC2-XSG11//TH70200 | 1350 PSI | 35044 | 2.5”x 4” | Yes | Outlet piping | Unified valve 6, 2013 |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas X | Water |
| Amine | LPG | Condensate | Air | Glycol |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | Vessel not insulated. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint in good condition on saddles – no exposed metal. |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks observed. |
| Saddle/skirt Assess condition of paint, fire protection, and concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Saddles: Bolted directly to skid deck. No buckling or dents. No corrosion at attachment welds to vessel. Ground wire attached to vessel. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Vessel saddles bolted firmly to skid deck – no deformation. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, and describe any hazards. |  |  |  | X |  |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | Flanged and threaded nozzle joints are fully engaged. No damage or deflections – no leaks. Nozzles are not gusseted. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | No gauges. |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Piping is well supported; no deflection, all clamps and supports are in place. Paint in good condition – no exposed metal. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | Valves are supported properly – no leaks. |
| PSV Ensure PSV is set at pressure at or below that of vessel. | X |  |  |  | Location: outlet piping – PSV removed for service. Block valve between vessel and PSV. Discharge piping is same size as valve out let. PSV seal in place |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic corrosion survey carried out Jan. 2013 – pipe metal thickness detected below nominal minus corrosion allowance. Thickness calculations carried out: UT point 255 (2” elbow) – nominal thickness is 5.5mm / min thickness is 4.0mm / T min thickness is 2.8mm. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: No recommendations. Summary: This vessel is in good condition, visual external and ultrasonic thickness inspection carried out – pipe metal thickness detected below nominal minus corrosion allowance. Thickness calculations carried out to ensure sufficient metal exists for safe operation. Vessel is fit for service. |

Inspected By: Gerry Avery			                                                                               Date: June 11, 2013

| Internal Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Coating Assess coating. Describe area coated, general condition of coating. | X |  |  |  | Coating in good condition – no blisters or chipped areas. Dry film thickness of coating no average 12 mils |
| Anodes. How many, type, condition. % consumed. Are they being replaced? |  |  |  | X | None. |
| Internal Piping Is there any? If so, carbon or stainless steel. Describe condition, dents, corrosion, erosion, etc. Ensure supports are secure and any bolts are suitable for future use. |  |  |  | X | None |
| Trays How many? Type of material. Are valves in place? Check for erosion/ corrosion; wear on tray valve legs. Cleanliness? |  |  |  | X | None |
| Baffles, deflector plates, etc. If present, describe condition. Look closely at welds attached to vessel wall. | X |  |  |  | Inlet deflector plate welded to top shell - plate coated no corrosion no staining or erosion noted. Vortex breaker welded in place – no mechanical damage – coated. |
| Top Head Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head) | X |  |  |  | Man way in good condition – no corrosion or chipped coating. Gasket seating face in good condition –no mechanical damage. |
| Bottom Head Note all corrosion, erosion or mechanical damage. (If vessel is horizontal identify direction of this head) | X |  |  |  | Back head in good condition – coated – no exposed metal. |
| Shell Sections Record number of shell sections. Record location, size and depth of all erosion, corrosion or mechanical damage. Describe general condition. If any corrosion greater than corrosion allowance is observed in either shell or head, discuss with Chief Inspector before closing vessel. | X |  |  |  | Nozzles are coated – no obstructions. Shell coated no blisters or chipped areas. No dents or mechanical damage to shell. |
| Demister pad Is it in place? Is it clean? If any corrosion is apparent in vessel, lift pad and check top head for corrosion. | X |  |  |  | Demister pad in place – clean – no open to torn sections. Support bars bolted in place. |
| Welds Inspect all welds, including attachment welds. Record all service-related damages and if there is any discuss with Chief Inspector before closing. | X |  |  |  | All welds are coated – no corrosion staining at welds. |
| Repairs Required. If yes, ensure procedure and copy of AB 40 is on file, and one sent to local ABSA, and Chief Inspector |  |  |  | X | None |
| NDE Was any NDE done. ( MI coordinator to review results) | X |  |  |  | Ultrasonic corrosion survey carried out, pipe metal thickness detected below nominal minus corrosion allowance. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: No recommendations at this time. Summary: Vessel is in overall good condition, visual external inspection and ultrasonic corrosion survey performed—pipe metal thickness detected below nominal minus the corrosion allowance. Thickness calculations carried out to ensure sufficient metal exists for safe operation. Vessel is fit for service. |

Inspected By: Gerry Avery			                                                                               Date: June 11, 2013

| Vessel data plate | Man way bolting flange |
| --- | --- |
| overview | Inlet nozzle |
| Vortex breaker | Inlet deflector plate |
| Demister pad | Demister pad support bars |
| Temperature probe | Internal overview |
| Man way | PSV data tag |
| PSV |  |