| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION Job # 05.003656 |
| --- |
| District: Grande Prairie AB | Skid No. |
| Facility: Bonanza Compressor Site | Location (LSD): 13-34-81-11 W6M |
| Vessel Name Equipment Number: Glycol Contactor |
| Orientation: Vertical |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. A 0431782 | CRN Number: M 2316.21 |
| Vessel serial number: 96-8664-4 | Size: 24 in. X 30 ft. |
| Shell thickness: 28.4 mm | Shell material: SA 516 70N |
| Head thickness: 27.9 mm | Head material: SA 516 70N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 1440 PSI | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 130 Deg F | Operating temperature | Shell: 0 – 250 Deg F |
|  | Tubes: |  | Tubes: |
| X-ray: RT 1 | Heat treatment: Yes |
| Code parameters: ASME VIII, Div 1 | Coated: no |
| Manufacturer: Wells-Hall Fabrication | Year built: 1997 |
| Corrosion allowance: 3.2 mm | Manway: no |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture | Model # | Serial # | Set Pressure (kPa) | Capacity (scfm) | Service Date |
| 5501G | Farris | 26FA13-1 20 | CE43148-2-A10 | 1200 PSI | 7774 | 09/07 |
| CRN # | Service By | Block Valve | Location | Size | Code Stamp |  |
| OG2369.5C | Unified valve | No | Lower shell | 1.5”x 2” | UV |  |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet | Sour X | Oil | Gas X | Water X |
| Amine | LPG | Condensate | Air | Glycol X |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | Vessel is not insulated. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint in good overall condition – no exposed metal. |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks observed. |
| Saddle/Skirt Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Skirt: bolted directly to skid floor. No buckling or dents. No corrosion at attachment welds to vessel. Ground wire attached to skid. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Anchor bolts are securely fastened. No deformation. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, describe any hazards. |  |  |  | X |  |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | Stud threads are fully engaged to nuts. No short bolting. No damage or deflections. Nozzles are not gusseted. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Clear and clean – no leakage. Suitable for range of MAWP/Temperature. Temperature gauge 0 – 250 Deg F. |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Piping is well supported. All clamps and supports are in place. No structural overloads or deflections. Paint in good condition – no exposed metal. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | No leaks are visible. Valves are supported properly. |
| PSV Ensure PSV is set at pressure at or below that of vessel. | X |  |  |  | Location: Lower shell – set below MAWP of vessel. Discharge piping is same size as valve outlet. PSV seal in place. No block valve between vessel and PSV. |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance. See summary for corrosion rate. |
| Other | X |  |  |  | Bore scope camera used to view bottom head and drain in glycol contactor – no pitting detected. Accessed through 3 in. nozzle on lower shell. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1. Ultrasonic thickness inspection should be carried out in 1 year time frame to better assess the corrosion rate in the lower shell area. Summary: Vessel is in overall good condition, visual external inspection and bore scope inspection through small bore fitting in lower shell – no pitting detected. Ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance. There appears to be an aggressive corrosion rate in the lower shell area - .028 inches per year. Vessel is fit for service. |

Inspected By: Gerry Avery			                                                                                            Date: October 1, 2009

Photo Table

| LSD | Vessel data plate |
| --- | --- |
| Vessel temperature gauge | PSV data tag |
| Vessel PSV | Vessel overview inside skid |
| Vessel overview | 3” nozzle access with bore scope |

|  | Applus RTD Canada 5504-36 Street Edmonton, Alberta T 780 440 6600 F 780 440 2538 www.applusRTD.ca | Ultrasonic Inspection Report | # GC-09181 |
| --- | --- | --- | --- |
|  |  | Date (m/d/y): | 10/01/2009 | Page | 1 | of | 1 |  |
|  |  | Applus RTD Job #: | 05.003656 |  |
|  |  | Applus RTD Dep. #: | ASSET |  |
| Client: | Canadian Natural Resources Ltd. |  | Job location: | Compressor 13-34-81-11-W6M |  |
| Address: | Grande Prairie, Alberta |  | Applus RTD Procedure(s): | UT-001 | Rev. #: | 2 |  |
|  |  |  | Code / Standard: | ASME SEC V/ASME SEC VIII |  |
| PO/WO: | NS |  | Client Specification: | ASME SEC VIII/CLIENTS REVIEW |  |
| Item Inspected: | Contactor A# 431782 |  |
| Method: | Zero Degree |  | Scanning Surface: | Outer Diameter |  |
| Type: | Manual |  | Surface Condition: | Painted / As Is |  |
| Instrumentation: | UT Flaw Detector | Manufacturer: | Panametrics | Type: | Epoch IV | Asset No: | 10307 |  |
| Calibration: | Due Date: | November /09 | Sheet #: | NiL | (Optional) Instrument Serial No.: | NIL |  |
| Calibration Block(s): | Type: | Metric Step Wedge | Asset No.: | 10823 | Type: |  | Asset No.: |  |  |
|  | Type: |  | Asset No.: |  | Type: |  | Asset No.: |  |  |
| Couplant: | Manufacturer: | SonoTech | Type: | UTX | Cable: | Type: | MICRODOT TO BNC | Length: | 4 FEET |  |
| Probe Type | Angle | Frequency | Size | Reference Level (dB) | Scanning Level (dB) | Range | Skip Value | Beam Travel | Transfer Value (dB) |
| DUAL | O | 5MHZ | 0.25 | 60db | 70db | 65MM | NIL | BACKWALL | NIL |
| Inspection Details |
| Scope: | To perform an ultrasonic thickness survey on the contactor A# 431782 looking for material wall loss areas and identifying as requested. (See drawings for survey locations) |
| Results: | The ultrasonic thickness survey was performed at the above described. Refer to Sept 2009 corrosion survey for details. No metal thickness detected below nominal minus corrosion allowance. UT thickness in 2004 – 29.3 mm UT thickness in 2009 – 25.8 mm This is a wall loss of 3.5 mm in 5 years – this is substantial as the service is sweet and glycol is circulated through the shell and bottom head area. Corrosion rate on the shell is - .7 mm per year / .028 inches per year. |
| Assistant 1: |  | Technician: | Greg Cook (CGSB Reg. #: 10584) |
| Assistant 2: |  |  | CGSB ASNT SNT Level: 1 2 3 |
|  | CGSB ASNT SNT Level: 1 2 | Discipline: | UT MT PT ET RT VT |
| Discipline: | UT MT PT ET RT VT | Signature: |  |
| Client Name: Craig Liba | Client Signature: |  | Date:(m/d/y) | 10/01/2009 |