| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION JOB#05.004093 |
| --- |
| District: Grande Prairie, Ab. | Skid No. |
| Facility: Thunder Creek Compressor Station | Location (LSD): d – 31 – H / 93 – I – 15 |
| Vessel Name & Equipment Number: Glycol Contactor |
| Orientation: Vertical |
| Status: Operating | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| Registration Number A 506261 | CRN Number P 5021.213 |
| Vessel serial number: 2004 – 7204 – 01A | Size: 24 in. OD x 30 ft. S/S |
| Shell thickness: 25.4 mm | Shell material: SA 516 70 N |
| Head thickness: 23.8 mm | Head material: SA 516 70 N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 9929 kPa | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 54°C | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: RT 1 | Heat treatment: HT |
| Code parameters: ASME VIII / Div 1 | Coated: No |
| Manufacturer: Alco Gas and Oil. | Year built: 2004 |
| Corrosion allowance: 3.2 mm | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag no. | Manufacture | Model | Serial number | Set Pressure | Capacity | Size |
| TCCS 014 | Farris | 26FA13 – 120 | CE-463640-5- A10 | 9929 kPa | 9328 scfm | 1.5 in. x 2 in. |
| Serv By | Date | Block Valve | CRN number | Code Stamp | Location |  |
| Farris | 06/2007 | No | OG 8442.5C | UV | Lower Shell |  |
| SERVICE CONDTIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas X | Water X |
| Amine | LPG | Condensate | Air | Glycol X |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of  CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site,  and copy sent to Chief Inspector

### A # 506261

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation: Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | Vessel is not insulated. |
| External Condition: Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) |  | X |  |  | Good condition – no exposed metal. |
| Leakage: Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks detected. |
| Skirt: Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Skirt: Separator is mounted firmly to skid deck, no distortion or buckles. No corrosion at head to shell weld – no leaks. Skid Package is grounded. |
| Anchor Bolts: Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Firmly bolted to skid deck. |
| Concrete foundation: Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform: Describe general condition, ensure support is secure to vessel, describe any hazards. |  |  |  | X |  |
| Nozzle: Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | All studs fully engaged to nuts – no short bolts. No deflection, no leaking detected. No gussets. |
| Gauges: Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Temp and pressure gauges firmly attached and within operational parameters for service. |
| External Piping: Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Well supported, no deflection, all clamps in place. Paint is in god condition – no corrosion. |
| Valving: Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | Firmly supported – no leaks. |
| PSV: Ensure PSV is set at pressure at or below that of vessel. |  |  |  |  | Located on lower shell, set below MAWP of vessel. Seal is intact. No block valve. Discharge piping is same size as outlet orifice. |
| NDE methods: Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic thickness survey carried out – no metal thickness detected below nominal minus corrosion allowance. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: No recommendations at this time. Summary: Vessel is in overall good condition, visual external inspection and ultrasonic corrosion survey performed – no metal thickness detected below nominal minus corrosion allowance. Vessel is fit for service. |

Inspected By:  D. Wiedman                                                                                                                                      Date: March 23, 2010

Glycol Contactor – A 506261