| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION Job# 05.004093 |
| --- |
| District: Grande Prairie, Ab. | Skid No. |
| Facility: Thunder Creek Compressor Station | Location (LSD): d – 31 – H / 93 – I – 15 |
| Vessel Name & Equipment Number: Line Heater |
| Orientation: Vertical |
| Status: Operating | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| Registration Number A 528515 | CRN Number P 9412.132 |
| Vessel serial number: BW 336.003 | Size: 48 in. OD x 15 ft. S/S |
| Shell thickness: 9.5 mm | Shell material: SA 36 |
| Head thickness: 9.5 mm | Head material: SA 36 |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 4651 kPa | Operating pressure | Shell: |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 38°C | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: RT 1 | Heat treatment: Nil |
| Code parameters: ASME B 31.3 | Coated: No |
| Manufacturer: Brooks Welding | Year built: 2005 |
| Corrosion allowance: 3.2 mm | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag no. | Manufacture | Model | Serial number | Set Pressure | Capacity | Size |
| 21767P TCCS 020 | Mercer | 8142251T23NS | 140256 | 4964 kPa | 5816 scfm | 2 in. x 2 in. |
| Serv By | Date | Block Valve | CRN number | Code Stamp | Location |  |
| Unified Valve | 06/2007 | No | OG 8441.5C | UV | Outlet Piping |  |
| SERVICE CONDTIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas X | Water X |
| Amine | LPG | Condensate X | Air | Glycol |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of  CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site,  and copy sent to Chief Inspector

### A # 528515

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation: Verify sealed around man ways, nozzles, no damage present, and there is no egress of moisture. | X |  |  |  | Vessel is fully insulated – no open or torn sections. No evidence of wet insulation – no stains. |
| External Condition: Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Good condition – no exposed metal. |
| Leakage: Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks detected. |
| Saddle: Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Saddle: This line heater is mounted on pilings and supports – no distortion to saddle – no evidence of leaking at saddle to shell area. Skid is grounded. |
| Anchor Bolts: Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Firmly bolted to skid deck. |
| Concrete foundation: Check for cracks, spalling, etc. |  |  |  | X |  |
| Ladder / Platform: Describe general condition, ensure support is secure to vessel, describe any hazards. |  |  |  | X |  |
| Nozzle: Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | All studs fully engaged to nuts – no short bolts. No deflection, no leaking detected. No gussets. |
| Gauges: Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Temp and pressure gauges firmly attached and within operational parameters for service. |
| External Piping: Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? | X |  |  |  | Well supported, no deflection, all clamps in place. Paint is in god condition – no corrosion. |
| Valving: Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | Firmly supported – no leaks. |
| PSV: Ensure PSV is set at pressure at or below that of vessel. |  |  | X |  | Located on Discharge Piping, set above MAWP of gas coil. Seal is intact. No block valve. Discharge piping is same size as outlet orifice. |
| NDE methods: Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic thickness survey carried out – shell metal thickness detected below nominal. Shell is atmospheric – general corrosion in vapor space but is minimal. Nominal is 9.5 mm – min thickness is 8.9 mm. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1. Re set PSV to MAWP of coil or below. Summary: This line heater is in overall good condition, visual external inspection and ultrasonic corrosion survey performed – shell metal thickness detected below nominal – general corrosion – no pitting. Vessel is fit for service. |

Inspected By:  D. Wiedman                                                                                                                                     Date: March 22, 2010