| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION Job # 05.002086 |
| --- |
| District: Fort St John, B.C. | Skid No. |
| Facility: South Bulrush Compressor Station | Location (LSD): b-88-F / 94-A-16 |
| Vessel Name Equipment Number: Inlet Separator |
| Orientation: Vertical |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. A 3098523 | CRN Number: M-2318.213 |
| Vessel serial number: 95-7975-0 | Size: 36 in x 10ft |
| Shell thickness: 22.2 mm | Shell material: SA 516 70MT |
| Head thickness: 27.8 mm | Head material: SA 516 70MT |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 720 PSI | Operating pressure | Shell: 0 PSI |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 100 deg F | Operating temperature | Shell: |
|  | Tubes: |  | Tubes: |
| X-ray: RT-1 | Heat treatment: Yes |
| Code parameters: ASME Sec VIII, Div 1 | Coated: No |
| Manufacturer: Wells Hall Fab. | Year built: 1995 |
| Corrosion allowance: 3.2mm | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture | Model # | Serial # | Set Pressure (kPa) | Capacity (scfm) | Service Date |
| 1225F | Farris | 26GA12-120/S7 | CE-41879-A10 | 720 PSI | 7081 | 07- 2004 |
| CRN # | Service By | Block Valve | Location | Size | Code Stamp |  |
| OG 2369.5C | Unified Valve | No | Discharge piping | 1.5” X 2.5” | UV/NB |  |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet | Sour X | Oil | Gas X | Water X |
| Amine | LPG | Condensate X | Air | Glycol |
| Other (Describe): |

# Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | No insulation. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Paint is in good overall condition – no exposed metal or surface corrosion. Newly painted. |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaking detected. |
| Saddle/skirt Assess condition of paint, fire protection, and concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Skirt is in good condition – no buckles or distortion. Paint intact – with corrosion. Vessel grounded through skid. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Firmly secured – no signs of deformation. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X | None. |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, and describe any hazards. |  |  |  | X | None. |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | All threads engaged. No deflection – no leaks. No gussets. Painting good overall condition. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. |  | X |  |  | Gauges are visible, appears to be functional, no leaks but the pressure gauge is not suitable for range. Temp gauge: -40-120 deg F. Pressure gauge: 0-300 PSI. |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? |  | X |  |  | Well supported – no deflection – all clamps and shoes in place. Piping is painted and is in fair overall condition with external surface corrosion to 30% - pitting to 0.010” max. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. | X |  |  |  | Well supported – no leaks. |
| PSV Ensure PSV is set at pressure at or below that of vessel. | X |  |  |  | Located on Gas Outlet Piping. Seal intact – No block valve. Outlet piping same size as orifice. PSV set at MAWP. |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic corrosion survey carried out, Pipe metal thickness detected below nominal minus corrosion allowance. Thickness calculations carried out to ensure sufficient metal exits for safe operation. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1) Install new pressure gauge with range that covers MAWP listed on data plate. Summary: This vessel is in good condition, visual external and ultrasonic thickness inspection carried out – pipe metal thickness detected below nominal minus corrosion allowance. Thickness calculations carried out to ensure sufficient metal exits for safe operation. Vessel is fit for service. |

Inspected By: Joe Holdstock				                                                                               Date: July 22 2008

|  | Data Plate Overview |
| --- | --- |
| Overview | Overview |
| External corrosion / Inlet Nozzle | External corrosion / Inlet piping |
| Pressure gauge | Temperature gauge |