| Canadian Natural Resources Limited GENERAL PRESSURE VESSEL INFORMATION |
| --- |
| District: Grande Prairie, AB | Skid No. |
| Facility: George Gas Plant | Location (LSD): 06-32-82-05 W6M |
| Vessel Name Equipment Number: Inlet Separator |
| Orientation: Vertical |
| Status: In Service | Regulatory Inspection |
| PRESSURE VESSEL NAMEPLATE DATA |
| “A” or “G” or “S” (Sask.) or BC Registration Number. A 2692854 | CRN Number: K-1186.2 |
| Vessel serial number: 04013 | Size: 24 in x 8 ft |
| Shell thickness: 28.6mm | Shell material: SA 516 70N |
| Head thickness: 28.6mm | Head material: SA 516 70N |
| Tube wall thickness: | Tube material: |
| Tube diameter: | Tube length: |
| Channel thickness: | Channel material: |
| Design pressure | Shell: 9929 kPa | Operating pressure | Shell: 0 -1000 kPa |
|  | Tubes: |  | Tubes: |
| Design Temp. | Shell: 38°C | Operating temperature | Shell: -20(C to 120(C |
|  | Tubes: |  | Tubes: |
| X-ray: RT-1 | Heat treatment: HT |
| Code parameters: Asme VIII, Div 1 | Coated: |
| Manufacturer: Bromley Mechanical Services | Year built: 1991 |
| Corrosion allowance: 3.2mm | Manway: No |
| PRESSURE SAFETY VALVE NAMEPLATE DATA |
| PSV Tag # | Manufacture | Model # | Serial # | Set Pressure (kPa) | Capacity (scfm) | Service Date |
| 18704G | Farris | 26FA13-120 | CE-42857-1-A10 | 9929 | 9317 | 2004 |
| CRN # | Service By | Block Valve | Location | Size | Code Stamp |  |
| 0G2369.5C | Unified Valve | No | Outlet Piping | 1.5” 600# x 2” 150# | UV/NB |  |
| SERVICE CONDITIONS-INDICATE ALL THAT APPLY |
| Sweet X | Sour | Oil | Gas X | Water |
| Amine | LPG | Condensate | Air | Glycol |
| Other (Describe): |

Inspection Interval ________________________________________PSV Service Interval_________________________________

# (Determined by MIC in conjunction with Chief Inspector following guidelines of  CNRL’s Owner-User Inspection Program)

Reports reviewed and accepted by:

# Mechanical Integrity Coordinator________________________________________________Date__________________________

# Fill out all forms as completely as possible. All information is important!  Use back of sheets to record additional information or sketch if required.

# Copy of report to be filed by MIC at site, and copy sent to Chief Inspector

| External Inspection Items | G | F | P | N/A | Comments |
| --- | --- | --- | --- | --- | --- |
| Insulation Verify sealed around manways, nozzles, no damage present, and there is no egress of moisture. |  |  |  | X | Vessel not insulated. |
| External Condition Assess paint condition, areas peeling, record any corrosion, damage, etc (record location, size and depth of corrosion or damage) | X |  |  |  | Minor paint chipping to <5% surface area. Abrasion mid shell approx. 12 inches, surface corrosion. No damage |
| Leakage Record any leakage at flanges, threaded joints, weep holes on repads, etc. | X |  |  |  | No leaks observed. |
| Skirt Assess condition of paint, fire protection, concrete. Look for corrosion, buckling, dents, etc. Look at vessel surface area near supports. Verify no signs of leakage at attachment to vessel and attachment welds are acceptable. Ground wire attached? | X |  |  |  | Skirt firmly bolted to skid floor. No evidence of leaking or seeping at base. Skirt/base paint in fair condition – minor corrosion on base plate. Skid is mounted at ground level on pilings Skid package is grounded. |
| Anchor Bolts Hammer tap to ensure secure. Look for cracking in treads or signs of deformation. | X |  |  |  | Vessel is firmly bolted. |
| Concrete foundation Check for cracks, spalling, etc. |  |  |  | X | Metal floor. |
| Ladder / Platform Describe general condition, ensure support is secure to vessel, describe any hazards. |  |  |  | X | None |
| Nozzle Assess paint, look for leakage, and ensure stud threads are fully engaged. Record any damage, deflection, etc. Are nozzles gusseted? | X |  |  |  | Threaded nozzle joints are fully engaged Stud on gas outlet flange not fully engaged. Nozzles are not gusseted. No damage. No deflections. No leaks Minor paint chipping to nozzles and flanges to 5% area. |
| Gauges Ensure gauges are visible, working, no leakage, and suitable for range of MAWP/ Temp. | X |  |  |  | Pressure, temperature and liquid level gauges attached Clean and clear. No leaks. Pressure gauge: 0 to 1500 psi - within range for service Temperature gauge: -20 to 120 (C - within range for service |
| External Piping Ensure pipe is well supported. All clamps, supports, shoes, etc. in place. Look for evidence of structural overload, deflection, etc. Paint condition, external corrosion? |  | X |  |  | Inlet piping approx 4 ft unpainted. Drain piping approx 2 ft unpainted. Remainder of piping chipped to 5% exposed metal. Well supported – all clamps in place. No overload or deflection. |
| Valving Ensure no leaks are visible. Valves are properly supported and chained if necessary. |  | X |  |  | Minor seepage at 1.5” produced water valve. |
| PSV Ensure PSV is set at pressure at or below that of vessel. | X |  |  |  | Located on outlet piping- set at MAWP of vessel. Discharge piping is same size as valve outlet. Valve is properly supported and routed. PSV seal in place. No block valve. |
| NDE methods Was UT/ MPI done on vessel (MI coordinator to review results) | X |  |  |  | Ultrasonic thickness survey carried out – pipe metal thickness detected below nominal minus corrosion allowance. Critical thickness calculations carried out to ensure sufficient metal exists for safe operation. |
| Recommendations or corrective actions : Vessel is Fit for Service or describe corrective actions required) (MIC to review corrective actions with Operations, discuss with Chief Inspector where necessary, and get remedial action implemented) Recommendations: 1. Adjust short bolted stud on outlet flange. 2. Paint unpainted piping. 3. Repair seeping valve. Summary: This vessel is in good overall condition – visual external and ultrasonic thickness inspection carried out - pipe metal thickness detected below nominal minus corrosion allowance. Critical thickness calculations carried out to ensure sufficient metal exists for safe operation. |

Inspected By: D. Wiedman / C. Maxsom                                                                                                              Date:  April 27, 2009

Photo Table

| LSD | Overview – Skid |
| --- | --- |
| Over view – Lower Shell and Piping | Overview – Upper Shell |
| Data Plate | Short bolted stud |
| Exposed Inlet piping | Seepage at valve |